## Slide 1
This patient presented with a failed restoration on endodontically-treated lateral incisor (#10). There is adequate tooth structure to restore with composite, rather than a crown
July, 2002
Clinical Case: DT Light-Post
Clinical case by:
Professor Dr. Alejandro Bertoldi Hepburn

## Slide 2
3. The depth of the post space is established using the universal starter drill, and the shape is finalized with the Finishing Drills.
5. A standard round post is tried- in. Note the profound remaining pace at the neck of the post.
6. The Macro-Lock OVAL post provides a better fit in the coronal section, leaving LESS CEMENT available to shrink.
4. Clearly, there is a exceptional flare toward the coronal opening of this space, and an OVAL opening.
1. Determine the post size using the size selection card provided in the kit.
2. Remove any obstruction and confirm the seal of the Gutta Percha.

## Slide 3
12. Inject Dual-cure cement, and immediately insert the post.
10. Etch the canal space and tooth structure according to manufacturer’s instructions.
7. Apply light-cured adhesive Bonding Agent to the post.
8. Air-dry to evaporate the solvent.
11. Apply Bonding resin to the surfaces.
Remove excess, air-dry. Light-cure.
9. Light-cure the bonding agent.

## Slide 4
The DT Light-Post has a double-tapered, anatomic design, to provide a good fit with minimal cement thickness.
In this case, there was sufficient remaining tooth structure to avoid full coverage prosthetics, and a post was added to provide support for the direct composite restoration. After the post was placed, the old restoration was removed and a new tooth built.
In vitro research indicates that the addition of a quartz fiber post in anterior endodontically-treated teeth provides a more durable restoration with better failure modes.
Products used in this case:
RTD DT Light-Post
Bisco Uni-Etch with BAC
Bisco One-Step Adhesive (5th Generation)
Affiliations:
Dr. Professor Bertoldi Hepburn teaches at Universidad de Desorrollo, Concepcion, Chile and Universidad de Buenos Aires, Argentina.